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PRODUCT INFORMATION

[bookmark: _Hlk169992110]MAXXOL MXX TOP QUALITY 
0W-20.0W-30.5W-20.5W-30.5W-40

[bookmark: _Hlk169992834]MAXXOL MXX TOP QUALITY 0W-20,0W-30,5W-20,5W-30,5W-40 series are multipurpose engine oil for formulating Passenger Car suitable ILSAC GF-6 and API SP performance levels. Specially formulated to protect high compression gasoline
direct injection engines delivering superior oxidative stability, deposit Control Low Speed Pre-Ignition
mitigation and Timing Chain Wear protection.
- Delivers fuel economy without compromising durability.
- Provides superior protection against engine sludge.
- Provides protection against Low-Speed Pre-Ignition and associated engine damage.
- Excellent clean dispersion and provides effective lubrication.
MAXXOL MXX TOP QUALITY 0W-20,0W-30,5W-20,5W-30,5W-40 series are suitable for use in automotive gasoline engines where the manufacturer recommends an API SP, ILSAC GF-6 lubricant.

	Performance Level
	Viscosity Grade

	API SP
ILSAC GF-6 
	SAE 0W20,0W30,5W20,5W30,5W40



	Typical Properties
	0W20
	0W30
	5W20
	5W30
	5W40

	Specific Gravity (15/4℃)
	0.846
	0.8445
	0.8478
	0.8573
	0.85

	Kinematic Viscosity (100℃, cSt)
	8.07
	9.5
	8.3
	10.5
	13.53

	Viscosity Index
	155
	155
	155
	155
	155

	Flash Point (℃)
	230
	230
	230
	230
	230

	Pour Point (℃)
	-45.0
	-45.0
	-39.0
	-39.0
	-39.0

	
	
	
	
	
	


· Values shown are typical and may vary
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