Integrating lubricant technologies

PRODUCT INFORMATION

MAXXOL MXX TOP QUALITY

0W-20.0W-30.5W-20.5W-30.5W-40

MAXXOL MXX TOP QUALITY 0W-20,0W-30,5W-20,5W-30,5W-40 series are multipurpose engine oil for formulating Passenger Car suitable ILSAC GF-6 and API SP performance levels. Specially formulated to protect high compression gasoline

direct injection engines delivering superior oxidative stability, deposit Control Low Speed Pre-Ignition

mitigation and Timing Chain Wear protection.

- Delivers fuel economy without compromising durability.

- Provides superior protection against engine sludge.

- Provides protection against Low-Speed Pre-Ignition and associated engine damage.

- Excellent clean dispersion and provides effective lubrication.

MAXXOL MXX TOP QUALITY 0W-20,0W-30,5W-20,5W-30,5W-40 series are suitable for use in automotive gasoline engines where the manufacturer recommends an API SP, ILSAC GF-6 lubricant.

| Performance Level | Viscosity Grade |
| --- | --- |
| API SP ILSAC GF-6 | SAE 0W20,0W30,5W20,5W30,5W40 |

| Typical Properties | 0W20 | 0W30 | 5W20 | 5W30 | 5W40 |
| --- | --- | --- | --- | --- | --- |
| Specific Gravity (15/4℃) | 0.846 | 0.8445 | 0.8478 | 0.8573 | 0.85 |
| Kinematic Viscosity (100℃, cSt) | 8.07 | 9.5 | 8.3 | 10.5 | 13.53 |
| Viscosity Index | 155 | 155 | 155 | 155 | 155 |
| Flash Point (℃) | 230 | 230 | 230 | 230 | 230 |
| Pour Point (℃) | -45.0 | -45.0 | -39.0 | -39.0 | -39.0 |

- Values shown are typical and may vary