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PRODUCT INFORMATION

MAXXOL MXO T-Gear 4/5 75W-90  GL-4/GL-5

[bookmark: _Hlk169826919]MAXXOL MXO T-Gear 4/5 75W-90  GL-4/GL-5 Premium quality synthetic gear oil specially designed for lubrication
highly loaded elements of transmissions and gearboxes of passenger cars. Provides smooth gear shifting at both extremely low and high temperatures. Has excellent anti-foaming properties. Thanks to highly effective anti-wear and extreme pressure
additives perfectly protect various transmission components from wear and scuffing. Has high antioxidant stability. Has a high viscosity index and, accordingly, a wide range operating temperatures.
MAXXOL MXO T-Gear 4/5 75W-90  GL-4/GL-5 Recommended for use in transmissions, synchronized gearboxes of passenger cars, transfer cases boxes of all-wheel drive vehicles containing cylindrical, conical and spiral-conical
gears. Excellent for lubricating components of cars, trucks and buses and light commercial trucks, including those containing hypoid gears, with recommendations for use of API GL-4 class oils. 
Can be used in units operating under moderate loads, requiring universal classes of gear oils API GL-4/GL-5.

	Performance Level
	SAE

	SAE 75W-90; API GL-4/GL-5
MIL-L-2105; MAN 341-1 Z2; MAN 341 TYPE MB; 
MB 235.11; ZF TE-ML 02В, 08, 17A
	75W90



	Typical Properties
	
	75W90

	Specific Gravity (15/4℃)
	
	0.8646

	Kinematic Viscosity (100℃, cSt)
	
	14.45

	Kinematic Viscosity (40℃, cSt)
	
	75.76

	Viscosity Index
	
	203

	Flash Point (℃)
	
	201

	Pour Point (℃)
	
	-45.0

	Copper Strip Corrosion (150℃, 3hr)
	
	1a


· Values shown are typical and may vary
	                                                                         
image6.png
@ www.maxxol.ru




image7.png




image8.png
sales@maxxol.ru




image9.png
@ www.maxxol.ru




image10.png




image1.png




image2.png




image3.png




image4.png




image5.png
sales@maxxol.ru




