Integrating lubricant technologies

PRODUCT INFORMATION

MAXXOL MXO T-Gear 4/5 75W-90  GL-4/GL-5

MAXXOL MXO T-Gear 4/5 75W-90  GL-4/GL-5 Premium quality synthetic gear oil specially designed for lubrication

highly loaded elements of transmissions and gearboxes of passenger cars. Provides smooth gear shifting at both extremely low and high temperatures. Has excellent anti-foaming properties. Thanks to highly effective anti-wear and extreme pressure

additives perfectly protect various transmission components from wear and scuffing. Has high antioxidant stability. Has a high viscosity index and, accordingly, a wide range operating temperatures.

MAXXOL MXO T-Gear 4/5 75W-90  GL-4/GL-5 Recommended for use in transmissions, synchronized gearboxes of passenger cars, transfer cases boxes of all-wheel drive vehicles containing cylindrical, conical and spiral-conical

gears. Excellent for lubricating components of cars, trucks and buses and light commercial trucks, including those containing hypoid gears, with recommendations for use of API GL-4 class oils.

Can be used in units operating under moderate loads, requiring universal classes of gear oils API GL-4/GL-5.

| Performance Level | SAE |
| --- | --- |
| SAE 75W-90; API GL-4/GL-5 MIL-L-2105; MAN 341-1 Z2; MAN 341 TYPE MB; MB 235.11; ZF TE-ML 02В, 08, 17A | 75W90 |

| Typical Properties |  | 75W90 |
| --- | --- | --- |
| Specific Gravity (15/4℃) |  | 0.8646 |
| Kinematic Viscosity (100℃, cSt) |  | 14.45 |
| Kinematic Viscosity (40℃, cSt) |  | 75.76 |
| Viscosity Index |  | 203 |
| Flash Point (℃) |  | 201 |
| Pour Point (℃) |  | -45.0 |
| Copper Strip Corrosion (150℃, 3hr) |  | 1a |

- Values shown are typical and may vary