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TURBO FX 0W30
Turbo FX 0W30 is a premium-grade, fully synthetic engine oil scientifically formulated to give you maximum engine clean up properties using special cleansing agents that actively and continuously lock away harmful dirt and deposits. Turbo FX 0W30has been expertly engineered to help prolong the life and maintain the efficiency of emission systems in diesel automobiles

Turbo FX 0W30 is made with a proprietary blend of leading edge components formulated to be fully compatible with the latest Diesel Particulate Filters (DPF's). Turbo FX 0W30 has been designed to help deliver outstanding performance and protection in conjunction with fuel economy benefits
Advantage : 

• Active cleaning agents

• Low Ash content

•∙ Energy Saving

•∙ Enhanced frictional properties

•∙ Excellent low temperature capabilities

	Performance Level
	
	Viscosity Grade

	API SN/ ACEA C2/ BMW LL-04
	
	SAE 0W30


MB 229.51/229.52, VW502/505, Dexos 2
	Typical Properties
	
	SAE 0W30

	Specific Gravity (15/4℃)
	
	0.8427

	Kinematic Viscosity (100℃, cSt)
	
	10.02

	Kinematic Viscosity (40℃, cSt)
	
	50.98

	Viscosity Index 
	
	188

	Flash Point (℃)
	
	226

	Pour Point (℃)
	
	-45

	CCS Viscosity (cP)
	
	5,780 (-35℃)

	TBN (mg·KOH/g)
	
	7.10

	TAN (mg·KOH/g)
	
	1.58


· Values shown are typical and may vary
