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TURBO DIESEL FX 10W40
Turbo Diesel FX provides maximum protection to both gasoline and diesel engines operating under severe service. Turbo Diesel FX is formulated with high-tech. additives system combined with premium quality, full synthetic base stocks and offers excellent performance in new RV and SUV as well as gasoline & diesel engines equipped with turbochargers or superchargers.

Advantages

· High Temperature Protection: Resist breakdown in the most severe engine environments

· Low Temperature Protection: Flows easily at low temperatures, reducing wear at start-up

· High Detergency: Fights formation of sludge and varnish deposits that reduce engine life

· Soot Dispersancy : Controls oil viscosity increase at high soot load

· Foam Control: Inhibit formation of foam under severe condition

· Wear Protection: Contains anti-wear additives that dramatically reduce engine wear

· Turbo Approved: Provides excellent protection to critical turbo unit component

· TBN Retention: Maintains acid-neutralizing capacity throughout lifecycle of oil
	Performance Level
	Viscosity Grade

	API CI-4/SL

ACEA E7

MB 228.3/229.1

Volvo VDS-3
Mack EO-M Plus

	SAE  10W40


	Typical Properties
	
	10W40

	Specific Gravity (15/4℃)
	
	0.8722

	Kinematic Viscosity (100℃, cSt)
	
	14.41

	Kinematic Viscosity (40℃, cSt)
	
	96.38

	Viscosity Index
	
	155

	Flash Point (℃)
	
	220

	Pour Point (℃)
	
	-36.0

	C.C.S (cP)
	
	6,450 (-25℃)

	TBN (mg·KOH/g)
	
	9.82

	TAN (mg·KOH/g)
	
	2.24


· Values shown are typical and may vary
