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TURBO DIESEL PLUS 15W40
TURBO DIESEL PLUS is a premium synthetic blend fuel economy and mixed fleet motor oil recommended for naturally aspirated and turbocharged four-stroke diesel engines and four-stroke gasoline engines in which the API CI-4 service category and SAE 15W-40 viscosity grade are recommended. This oil is especially suitable for heavily loaded diesel engines.
Benefits of TURBO DIESEL PLUS include:
• High detergency and superior dispersibility keep engines clean and soot suspended in the oil despite longer drain intervals and increased soot loading.
• Superior anti-wear agents extend engine life despite high operating temperatures and extended service intervals.
• Exceptional resistance to thermal degradation, even under the most severe operating temperatures, prevents viscosity increase and the deposit formation and wear that can result.
• Highly reliable performance over a wide range of temperatures, including severe cold.
	Performance Level
	Viscosity Grade

	API CI-4/SL

ACEA E7

MB 228.3/229.1


	Volvo VDS-3
Mack EO-M Plus

	SAE 15W40


	Typical Properties
	
	15W40

	Specific Gravity (15/4℃)
	
	0.8758

	Kinematic Viscosity (100℃, cSt)
	
	14.07

	Kinematic Viscosity (40℃, cSt)
	
	107.1

	Viscosity Index
	
	141

	Flash Point (℃)
	
	231

	Pour Point (℃)
	
	-35.0

	C.C.S (cP)
	
	6,050 (-20℃)

	TBN (mg·KOH/g)
	
	8.73

	TAN (mg·KOH/g)
	
	2.18


· Values shown are typical and may vary
